The Using Direction of Ink Jet CTP Plate

Ink jet CTP printing plate (positive) pushed out by our company for printing industry is dedicated for realizing computer-to-plate making on ink jet platesetter.

Positive Ink Jet CTP Plate:

Based on the conventional positive PS plate which use specialized aluminum plate as its substrate, ink jet CTP plate is coated with ink receiving layer. After the documents been processed by computer and then printed with ink, the plate are to be made by exposing above the glass of vacuum printer(no need vacuum pumping), and then washing, developing or by constant exposure and wash and then automatically developing.

Ink jet CTP plate does not use films,and are mainly applied in printing of text and low & medium color printing (4 colors).

The applicable ink jet system: EPSON, ROLAND, MIMAKI, MUTON and other micro  piezoelectric systems.

Using direction:

1. Open the package and then fetch out the plate with your two hands grabbing the two sides of the plate, avoiding to touching the plate face.

2. In case the wrong printing, you must insert the plate to the right place of the ink jet platesetter. The printing ink should be fast-drying pigment ink and dye ink.

3. Exposure: expose immediately after the plate is printed, or else may be distortion of the dot and line. If the relative humidity is relatively large, the printing plate can not be timely sulfate, this does not affect exposure, but before the exposure process is completed, any object touching the graphic part of the layout should be prohibited to prevent the text loss, then lead expose failed.Expose the printed plate above the glass of the printer, contral the expose time according to the form below:. (details depends on the degree of aging of the exposure machine, and during expose, couldnot get bubble on the plate, or else expose fail):

|  | 1kw | 2kw | 3kw | 4kw |
| --- | --- | --- | --- | --- |
| 0.6M | 50second | 25second |  |  |
| 1.0M | 65second | 40second | 20second |  |
| 1.2M | 70second | 50second | 30second | 15cond |
| 1.3M | 80second | 55second | 35econd | 20econd |

4. Wash :Wash off the printing layer of the printed plate immediately, with the running water under the normal temperature (temperature no lower than 25℃ ,using water of 40℃ will be better) and then wipe with the sponge which is special for printing plate, and then flush the front and back sides of the plates.

5. Develop:  The same operation with conventional positive PS plate. (The developer concentration should be 1:4, it’s up to the actual practice). Please do not touch the image area after developing and make sure to wash out the plate,and no residue of the developer.Make sure no developer left, then use the plate gum.

6. You can move to printing after the above process.

Storage condition and using environment:

1. Storage condition: (better to have dehumidifier or air conditioner)

- This printing plate should be stored in dry warehouse with dehumidifier, avoiding being damp.

- Storage temperature: ≤30℃, humidity: ≤60%

- Life time: 12 months

2. Using environment: (better to have dehumidifier or air conditioner)

- Operated under safe yellow light, temperature ≤30℃, humidity: ≤60%

- When unpacking the carton, please use up as soon as possible to avoid being damp

- In case being affected by sweat from hand, please touch the printing plate with gloves on