Pad printing (also called tampography) is a printing process that can transfer a 2-D image onto a 3-D object. This is accomplished using an indirect offset (gravure) printing process that involves an image being transferred from the cliché via a silicone pad onto a substrate

### Plate and ink interface technologies

#### Open inkwell system

Open ink well systems, the older method of pad printing, used an ink trough for the ink supply, which was located behind the printing plate. A flood bar pushed a pool of ink over the plate, and a doctor blade removes the ink from the plate surface, leaving ink on the etched artwork area ready for the pad to pick up.

#### Sealed ink cup system

Sealed ink cup systems employ a sealed container which acts as the ink supply, flood bar and doctor blade all at the same time. A ceramic ring with a highly polished working edge provides the seal against the printing plate.

### Printing pad

Pads are three-dimensional objects typically molded of silicone rubber. They function as a transfer vehicle, picking up ink from the printing plate, and transferring it to the part (substrate). They vary in shape and diameter depending on the application.

There are two main shape groups: "round pads" and long narrow pads called "bar pads". Pads are also made in other shapes, called "loaf pads". Within each group there are three size categories: small, medium, and large size pads. It is also possible to engineer custom-shaped pads to meet special application requirements.

### Image plate

Image plates are used to contain the desired artwork "image" etched in its surface. Their function is to hold ink in this etched cavity, allowing the pad to pick up this ink as a film in the shape of the artwork, which is then transferred to the substrate.

There are two main types of printing plate materials: photopolymer and steel. Photopolymer plates are the most popular, as they are easy to use. These are typically used in short to medium production runs. Steel plates come in two forms: thin steel for medium to long runs, and thick steel for very long runs. Both steel plate types are generally processed by the plate supplier as it involves the use of specialized equipment.

### Printing ink

Ink is used to mark or decorate parts. It comes in different chemical families to match the type of material to be printed (please consult the substrate compatibility chart for selection).

Pad printing inks are "solvent-based" and require mixing with additives before use. They typically seem dry to the touch within seconds although complete drying (cure) might take a substantially longer period of time. There are many more options. Inks that cure via the use of Ultra Violet light are convenient for certain applications. UV inks will not fully cure until UV light hits the ink. UV curable ink can be wiped off many substrates when mistakes are made. They can be cured with UV light in as fast as 1 second of light exposure. This depends on the ink, substrate and the light power and spectrum. UV inks can be reused as the pot life can be high as long as the ink stays clean, blocked from UV light and hasn't broken down from sitting. This same feature makes it easier to clean than some solvent and epoxy like two part component inks. Also there are heat curable inks, which work in much the same way as UV in the sense that there is a "trigger" that cures the ink when pulled. Two part inks usually have a pot life of only a few hours or so. They must be disposed of when they cannot be revived (by means of retarders etc.)

Climatic conditions will significantly affect the performance of any pad printing ink, especially the open ink well style printers. Too dry conditions can lead to faster evaporation of solvents causing the ink to thicken prematurely and too much moisture can lead to ink issues of "clumping" or something alike. Also the climate can affect other aspects of the printing process such as ink pick up and release from the plate to the pad to the substrate, as well as polymer plate to blade chattering or binding due to humidity.

### Substrate

Substrate is the technical term used to address any parts or materials to be printed. Fixtures vary in materials and complexity depending on the application. Substrates need to be clean and free from surface contamination to allow proper ink adhesion.

## Printing application examples

- Medical devices (surgical instruments, etc.)

- Implantable & in body medical items (catheter tubes, contact lenses, etc.)

- Golf ball logos/graphics

- Hockey Pucks[1]

- Decorative designs/graphics appearing on Hot Wheels or Matchbox toy cars

- Automotive parts (turn signal indicators, panel controls, etc.)

- Letters on computer keyboards and calculator keys

- TV and computer monitors

- Identification labels and serial numbers for many applications

Pad printing system package