Urea Moulding Compound Usage: 1.Spares of electrical appliance spares: switch, sockets. 2.Machinery spares: knob, handle, spinning machine components, instrument shell, clock shells. 3.Ornaments: Imitation pearls, buttons and pins. 4.Vessel: Various kinds of commercial used bottles, boxes and covers. 5.Others: toys, Mahjong cards, chess, ashtrays, balls, and toilet cover seats. Technical Specification: to 13454-92 Standard No. Index Unit Type Testing Method UF1P-C UFIG-C 1 Appearance Powdery Granular, with little powder After moulding, the surface should be flat, shinny and smooth, no bubbles or crack, color and residue match the sample 2 Resistance to boiling water no mushy, permit little color fade and purse GB13454 3 Gravity d2525,≤ 1.6 GB1033 4 Specific volume ml/g≤ 3 2 5 Volatile matter %,≤ 5.00 GB13455 6 Water absorb(cold) mg,≤ 100 GB1034 7 Shrinkage % 0.60-1.00 GB13454 8 Distortion Temperature ℃≥ 115 GB1634 9 Fludity mm 140-200 GB13454 10 Impact Strength(notch) KJ/m2,≥ 1.8 1.7 GB1043 11 Bending Strength Mpa,≥ 85 75 GB9341 12 Insulation Resistance after 24h in water MΩ≥ 104 GB1410 13 Dielectric strength MV/m,≥ 9.0 GB1408 14 Baking Resistance GRADE I GB2407

Moulding condition: (Reference only) Temperature 140-150℃ Pressure 25-40Mpa Curing time 0.5-1.0min/mm Packaging: Plastic knitting bag with inner one to two layer thin film bags. 25kg/bag Storage: Kept in airy, dry and cool room. Storage period: six months from the manufacturing date. Test should be undertaken when expires. Qualified products can still be used. Transportation Caution: avoid moisture, heat, dirt and packaging damage