－Melamine Moulding Compounds－

Properties: Using melamine formaldehyde resin as base material, a-cellulose as filling, adding pigments and additives brings about MMC. With good water resistance,high temperature resistance and non toxic.

| NO. | INDEX | UNIT | TYPE | TESTING METHOD |
| --- | --- | --- | --- | --- |
|  |  |  | MF1P-C | UFIP-B |  |
| 1 | Appearance |  | After moulding, the surface should be flat, shinny and smooth,no bubbles or crack, color and residue match the sample |  |
| 2 | Resistance to Boiling water |  | no mushy, permit little color fade and purse | GB13454 |
| 3 | Gravity | d2525,≤ | 1.6 | GB1033 |
| 4 | Specific volume | ml/g≤ | 3 |  |
| 5 | volatile matter | %,≤ | 5 | GB/T13455 |
| 6 | water absorb (cold)/(hot) | mg,≤ | 50 65 | GB1034 |
| 7 | shrinkage | % | 0.5-1.00 | GB13454 |
| 8 | Distortion temperature | °O,≥ | 155 | GB1634 |
| 9 | Flowing | mm | 140-200 | GB13454 |
| 10 | Impact Strength(notch) | KJ/m2,≥ | 1.9 | GB1043 |
| 11 | Bending Strength | Mpa,≥ | 80 | GB9341 |
| 12 | Insulation Resistance after 24h in water | MΩ≥ | 105 | —— | GB1410 |
| 13 | Dielectric strength | MV/m,≥ | 9.0 | —— | GB1408 |
| 14 | Baking resistance | GRADE | I | —— | GB2407 |
| 15 | distilled formaldehyde | mg/l | —— | 10.0 | GB5009，61-85 |
| Explanation | food health standard |  | After reasonable cure, MF1P-B willbe made into finished products of measuring GBn87-80 |

GBn87-80 According to health standard of Cyanuramide moulding finshed product.

| Index Name | Index,mg/l |
| --- | --- |
| Vaporize Residue(water) KMNO4 consumpation(water) formaldehyde (4% acetic acid) heavy metal(4% acetic acid) | 10 10 30 1 |
| color fade test | alcohol marinate cold food oil & colorless oil | negative |

Moulding condition(Referance only)

| Temperature | 150-160℃ |
| --- | --- |
| Pressure | 25-40Mpa |
| Curing time | 0.5-1.0min/mm |

Packaging: Plastic knitting bag with inner one to two layer thin film bags, 25kg/bag.
Storage: Kept in airy, dry and cool room.
Storage period: six months from the manufacturing date. Test should be undertaken when expires. Qualified products can still be used.
Transportation Caution: avoid moisture, heat, dirt and packaging damage.