NPP-688-FC / FW

Foaming Paste

Character

- For coloring, pigment is allowed to be added, the dosage depending on conditions.

- It is a ready-to-use paste which can be used directly, no need transparent rubber paste or binder to reduce the viscosity.

- NPP688FC / FW provide great foaming evenness, strong elasticity, washing duration and foam effect.

Application

Reference formula: Low foaming High foaming NPP-688-FC/FW Print one time Print two times Pigment --adding dosage subject to need Suitable for screen with 100~150 mesh. Suggested curing condition: 1) 150℃ for 10~12 seconds by Heat Presser or 2) 120~130℃ for 60~90 seconds by Oven. Suggested to be pre-dried at 60℃ or naturally dried under room temperature for 1~2days to obtain best results. Heating source could be “Oven”, “Infrared Ray Dryer” or “Iron”. “Steam Heater” is not allowed due to the coating will be impacted and lessen washing duration. Foaming failure may be caused by insufficient curing time.

Specification

- Appearance				：White Paste.

- Main Ingredients		：Macromolecular Polymer and Water

- PH  Value				：8 ± 1

- Package					：Net Weight 50KG / PE Drum

- Safety					：Avoid the direct touch of skin and eyes.

- Storage					：Keep container airtight and away from fire.

Store it in a cool(10°C~32°C), dark, and ventilated

place.

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.