NPP-651-Series

Discharge Paste

NPP-651-Series is an ECO discharge transparent / white paste, suitable for 100% cotton fabric.  It provides high color brightness, soft hand feel and also excellent washing fastness.  Steaming or soaping wash process is not required after printing.

Character

Application

- Use Directly.

- Discharge powder and thickener are mixable with NPP651 Series

upon conditions.

- Suggested curing condition is around 150~170℃ for 3~4 min

- Able to print lots of colors by adding various pigments. Adding dosage is

about 1~2%.

Specification

| Appearance | ：Milky white or White Paste. |
| --- | --- |
| Main Ingredients | ：Macromolecular Polymer, Water. |
| PH Value | ：Acidity |
| Package | ：Net Weight 50KG / PE Drum. |
| Safety | ：Avoid the direct touch of skin and eyes. |
| Storage | ：Keep container airtight and away from fire. Store it in a cool(10°C~40°C), dark, and ventilated place. |

Memo

NPP-621-Series is an ECO discharge transparent / white paste, suitable for 100% cotton fabric. It provides high color brightness, soft hand feel and also excellent washing fastness.  Steaming or soaping wash process is not required after printing.