NPP-300-ED

Elastic Semi-Discharge Paste

Character

Application

- Add the pigment resin color (6~8% depends on customer’s requirement)

and NPP rubber series to the NPP300ED directly, and stir the mixture well

for direct printing.

- To be applied on knitted fabric, good color developed effect especially for dark fabrics

- Provide soft hand-touch and excellent elasticity.

- Allow to be added with DE-03 Cross-linking agent / fixer or Binder to

increase the washing fastness if necessary

Specification

| - Appearance |  |  | : | Milk White Paste |  |
| --- | --- | --- | --- | --- | --- |
| - Solid content |  |  | : | 50% ± 2% |  |
| - Main ingredients |  |  | : | Acrylic Resin, Semi-discharge Powder |  |
| - PH value |  |  | : | 6 ~ 8 |  |
| - Storage |  |  | : | 12 months at cool shady place |  |
| - Package |  |  | : | 50KG/PE drum |  |

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.