NPP-541-W

White Rubber Paste for Nylon

NPP-541-W is the white paste for printing usage which is mainly applied for general fabrics (cotton, Polyester, Nylon…etc.). It provides excellent adhesive fastness and elasticity, especially suitable for the fabrics with poor adhesion like Nylon and Leather. Furthermore, BW-541 provides excellent shelter effects which especially works well with screen on direct-printing.

Character

- Non-tacky.

- Excellent washing fastness.

- Flat surface. - ECO-Friendly.

Application

- Allow to be added with DE Cross-linking agent or fixer to increase the washing fastness.

- Mixing with PRC series is highly recommended to produce accurate and bright colors

- Suitable for screen with less 120 mesh.

Specification

| - Appearance |  | ：White Paste. |  |  |
| --- | --- | --- | --- | --- |
| - Main Ingredients |  | ：Macromolecular Polymer, Water. |  |  |
| - PH Value |  | ：7 ± 1 |  |  |
| - Package |  | ：Net Weight 50KG / PE Drum. |  |  |
| - Safety |  | ：Avoid the direct touch of skin and eyes. |  |  |
| - Storage |  | ：Keep container airtight and away from fire. Store it in a cool (10°C~40°C), dark, and ventilated place. |  |  |

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.