NPP-541-FT

Foiling Transfer Paste

NPP-541-FT is a self cross-linking type PU copolymer hot-melt glue.  It is a reactive type emulsion providing high linking and high density properties,  specially suitable for imprinting on cotton fabric to obtain excellent adhesion for foiling.

Character

Excellent adhesion.

Superior washing resistance.

Application

- Direct use on printing, suitable for screen with 60~80 mesh

- Suggested curing temperature is 90~120℃ for 60~180 seconds or

naturally dried. Better to conduct transfer within 1~2days after printing

to obtain the best transfer results.

- For foil transfer, suggested heat pressing condition is 150~170℃ for

12~15 seconds with pressure around 3~4kg. Suggested condition

should be adjusted according to on site machines, operation and weather.

- BGE-208 Blocking Agent is allowed to be added to slow down paste drying

ate for easy operation, suggested dosage is within 3%.

- Cross-linking agent could be added for better adhesion and washing

resistance.

Specification

| Appearance | ：Slightly White Paste. |
| --- | --- |
| Main Ingredients | ：Macromolecular Polymer, Water. |
| PH Value | ：8 ± 1 |
| Package | ：Net Weight 50KG or 30KG / PE Drum. |
| Safety | ：Avoid the direct touch of skin and eyes. |
| Storage | ：Keep container airtight and away from fire. Store it in a cool (10°C~40°C), dark, and ventilated place. |

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.