NPP-702-C

Burn Out Paste

NPP-702-C is a paste applied to burn out the cotton fibers on T/C or CVC fabrics for transparent effect, the polyester fibers left is white and smooth.

Character

Application

Applied for screen printing directly. Water is allowed to be added to reduce viscosity to weaken burn out effect. Suggested to be cured at 170℃ 3Mins. Washing are required after printing.

Specification

- Appearance				：Slightly Milky White Paste

- Main Ingredients		：Macromolecular Polymer and Water

- PH  Value				：Alkaline

- Package					：Net Weight 50KG / PE Drum

- Safety					：Avoid the direct touch of skin and eyes.

- Storage					：Keep container airtight and away from fire.

Store in a cool (10°C~40°C), dark, and ventilated

place.

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.