NPL-9800-JC

3D Jelly Clear Plastisol Ink

Character

- High Transparency, High Brightness.

- Cured at higher temperature for better effect

- Phthalates free.

Application

Stir well before printing. Curing at 150℃in 3Mins after high-density printing to obtain vertical-angle effect. Curing at 180℃ 3Mins after high-density printing to obtain round effect. Mixing with glitter powder can make 9800-JC as an alternative solution to traditional glitter paste, and can largely improve the brightness. Allowed direct-printing just like transparent plastisol paste if collocated with NPC series. Providing excellent effect while works with thick screen printing.

Specification

- Appearance				：Slightly Yellow Transparent Paste.

- Main Ingredients		：Macromolecular Polymer, Disperse Agent,

Surfactants, Thickener.

- Package					：Net Weight 20KG / PE Drum.

- Safety					：Avoid the direct touch of skin and eyes.

- Storage					：Keep container airtight and away from fire.

Store it in a cool (10°C~40°C), dark, and

ventilated place.

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.