NPL-7550W/C

ECO White / Transparent Plastisol Ink

NPL-7550 is an eco friendly white plastisol ink, free from any restricted substances, easy to use, suitable for different kinds of fabric.

Character

- Soft feel and superior elasticity

- Excellent opacity

- Great transparency

- Phthalates free, meet various Environmental requirements.

- Low temperature dry

Application

- Mixing with NPC series color paste is highly recommended to produce accurate colors. - Ready-made ink used directly - Drying at temperature 150 degree C in 3 minutes, it’s adjustable upon conditions such as weather and machines’ type.

Specification

- Appearance				：White / Transparent Paste.

- Main Ingredients		：Macromolecular Polymer.

- PH  Value				：Neutral

- Package					：Net Weight 20 / 25KG PE Drum.

- Safety					：Avoid the direct touch of skin and eyes.

- Storage					：Keep container airtight and away from fire.

Store it in a cool (10°C~40°C), dark, and

ventilated place.

Memo

All recommendations are given only for reference; we do not guarantee the results of operation of which we have no direct control.  For further request, please contact to our technician for best solution.